## Slide 1: Formation of Deformation Twins in Metallic Crystals
S. Mahajan
Department of Materials Science and Engineering
University of California, Davis, 95616

## Slide 2: Formation of Deformation Twins in BCC Crystals

## Slide 5
Models Proposed for Formation of Deformation Twins in BCC Crystals
Pole Model of Cottrell and Bilby (1951)
½ <111>  1/3 <112> + 1/6 <11> ・
Note that the Burgers vector of the twinning partial, 1/6 <111> is not parallel to that of the parent slip dislocation.
Sleeskyk’s Model (1963)
  ½ <111> screws  3 1/6 <111> ・
  Note that the Burgers vector of the twinning partial, 1/6 <111>, is parallel to that of the parent slip dislocation

## Slide 6
Schematic of the Pole Model (Cottrell and Bilby)

## Slide 9: Case I
Habit Plane of F1, F2, F3, F4, and F5
They are all twins lying on the (211) plane;
F3 and F4 appear to be twins 3n layers thick.
Displacement Vector the Faults
Fault contrast visible for = 1 and invisible for = 01 and 110.
Therefore, the displacement vector is ± 1/6[11].
Burgers Vector of dislocations D1, D2, and D3
Visible for = 1
Invisible for = 01 and 110
Therefore, the Burgers vector is ± ½[1].
Conclusion
The Burgers vector of fault partials is parallel to that of the glide dislocations.
½[1]screws  3 x 1/6[1]

## Slide 11: Case II
Habit Plane of F6, F7... F16 (121)
Displacement Vector of Various Faults
Fault contrast is visible for = 10 and 00 and
invisible for = 1 and 12 and only the partials bounding
F6, F7, F14 and F16 are visible for = 12 ;
It is concluded that the displacement vector is ± 1/6[11].
Burgers vector of Dislocations D4, D5...D9
In contrast for = 10, 00 and 12
Invisible for = 1
Therefore, the Burgers vector is ± ½[11]
Conclusion
The Burgers vector of fault partials is parallel to that of the glide dislocations.
½[11]screws  3 x 1/6[11]

## Slide 12
Formation of ‘Clear’ Faults

## Slide 15
Spinodal Decomposition in Fe-Cr-Co Alloy
Grain Boundary
Precipitates

## Slide 18: Effects of Metallurgical Variables on Deformation Twinning in BCC Crystals

## Slide 19: Metallurgical Variables
Critical resolved shear stress for twinning
Deformation temperature
Strain-rate
Alloying

## Slide 20: EBSD Study of Twins in Shock Loaded Iron
Normal to
plane trace
Coincident
K1 poles
Coincident
Ƞ1 directions
Pole figures identifying {112}<111> twins
Multiple variants of the 60°@<111> twins
Orientation change along twins, indicating deformation
Crystal direction maps
Misorientation along black arrow

## Slide 21: Formation of Deformation Twins in FCC Crystals

## Slide 23
Pole Model (Venables)

## Slide 24
Formation of Fault Pairs

## Slide 32: Orientation Dependence of FCC Twinning

## Slide 34: Formation of {111} Twins in HCP Cobalt Single Crystals

## Slide 35: Governing Reactions 2 x <11 > + <100> → 12 x < [2 [110] → [100]

## Slide 36: Summary and Conclusions
Slip precedes deformation twinning in BCC, FCC and HCP structures
Embryonic twins evolve from dislocations
Microscopic twins form when stress-induced coalescence of embryonic twins occur that are located at different levels within micro-slip bands
Influence of metallurgical variables on deformation twinning can be rationalized in terms of the proposed models